Nature, 18 June 2008
http://www.w2agz.com

---
Electronic Structure of Rocksalt Copper Monoxide
Paul M. Grant
Visiting Scholar, Stanford University
Principal, W2AGZ Technologies
http://www.w2agz.com
Stanford Collaborators:
Ted Geballe
Bob Hammond
Mac Beasley
Gert Koster
Wolter Siemons
Con grazie mille e speciale a:
Paolo Gianozzi, Udine
Matteo Cococcioni, U Minn
Nicola Marzari, MIT
Axel Kohlmeyer, U Penn
Evyaz Isaev, MISA
Tone Kokal, Ljubljana
...e tutto di consorzio “Quantum Espresso,” ICTP

---
22 Years Ago...
...Still No Theory!

---
Bednorz-Mueller Nobel Lecture
After Chakravarty, (1979)

---
Cu2+ 3d Multiplet Splitting (Cubic)
Cu2+ 3d Multiplet Splitting (Cubic)
3d9
t2g
eg
Cu2+ Ion
Cubic

---
Hubbard Theory

---
Mott-Hubbard Insulator
Mott-Hubbard Insulator
After Imada, et al, RMP 70, 1039 (1998)

---
Charge Transfer Insulator
Charge Transfer Insulator
After Imada, et al, RMP 70, 1039 (1998)

---
Cubic Rocksalt Divalent TMOs
TMO	3d Config	Properties
MnO	5	MH-CTI (5.6)
FeO	6	MH-CTI (5.9)
CoO	7	MH-CTI (6.3)
NiO	8	MH-CTI (6.5)
CuO	9
XX Doesn't Exist!
See Imada, Fujimore, Tokura, RPM 70 (1988)

---
Néel Temperature vs. TMO Atomic Number

---
Tenorite (Monoclinic CuO)‏
Cu
O

---
DFT & (LDA + U)
DFT & (LDA + U)
Implemented in LMTO by Anisimov, et al, JPCM 2, 3973 (1990)
  - Applied to NiO, MnO, FeO, CoO and La2CuO4
Plane-Wave Pseudopotential Implementation by Cococcioni and de Gironcoli, PRB 71, 035105 (2005)
  - Applied to FeO and NiO
  - Download open-source package from http://www.pwscf.org

---
nm & af Unit Cells
a'
c
a
c'

---
af_0_pmg (U = 0)
eV
Z
Γ
A(X)
M
Y
Γ

---
af_5_pmg (U = 5)
eV
Z
Γ
A(X)
M
Y
Γ

---
Proto-TMO AF Rock Salt
Proto-TMO AF Rock Salt
[111]

---
Proto-TMO AF Rock Salt
[-1-1-1]

---
Cubic Rocksalt CuO

---
Cubic Rocksalt CuO (Cu 4s & O2p)

---
Comparison of Tenorite (111) to  CuO – MgO Proxy (100)
Comparison of Tenorite (111) to
CuO – MgO Proxy (100)
O
O
O
Cu
Cu
Cu
(111) Tenorite
(100) MgO
[Speaker Notes: This figure shows the possible growth interface for the lattice of monoclinic CuO matched to an MgO substrate. The Cu and O “yellow lines” on the “unfolded” interface suggest how the growth of cubic CuO might indeed begin on the (100) surface of MgO. The terms (111) and (100) are the “Miller indices” describing the intersection of symmetry planes with the crytallographic axes of tenorite and MgO respectively.]

---
Tetragonal CuO
Tetragonal CuO
c/a = 1.36
Measurements
(Wolter Siemons)
2-4 ML epi on STO
No Fermi Edge
No Exchange Bias on ferro-SRO (Tc ~ 100-150 K)
5.320
3.905
3.905

---
Cu2+ 3d Multiplet Splitting (Tetra)
Cu2+ 3d Multiplet Splitting (Tetra)
3d9
Cu2+ Ion
Cubic
Tetragonal
t2g
eg

---
Cubic
Tetragonal

---
Spin Composition of Cu 3d pDOS as fn(Hubbard)
Spin Composition of Cu 3d pDOS as fn(Hubbard)
U = 5 d-spin-pdos Cu1
U = 0 d-spin-pdos Cu1

---
t-CuO Density-of-States
t-CuO Density-of-States
E (eV)
EF
N(E) (eV-1)
He I UPS Spectrum
W. Siemons (PhD Thesis, Stanford)

---
Cubic & Tetragonal CuO
Ground State Properties
af-CuO
Total Energy + 233 Ry
Tetragonal Distortion, c/a
E(Ry)
Total GS Energy
af-CuO
N(Ef) vs c/a
TetragonaL Distortion, c/a
states/eV
DOS at Fermi Energy

---
Anharmonic Phonon-Driven HTSC?
“Fluctuating Cu-O-Cu bond model of
high-temperature superconductivity,”
D. M. Newns and C. C. Tsuei, Nature Physics 3, 184 (2007)

---
Conclusions & Homework
Conclusions
Rocksalt CuO can be used as a proxy material to study HTSC
Cubic RS CuO is a metal independent of U, subject to J-T distortions
Homework
Compute e-p coupling as fn(c/a,U), then 
Compute µ*, TN
Compute D , then TC
Look for anharmicities a la Newns & Tsuei